## Slide 1
HGX Series
SGSO Technology
Notes: Sustained Growth Smart Optimization

## Slide 2
HGX (ATX coating - Nano Multiple layer structure)

## Slide 3
HSX/HGX coating- Nano Coating
Competitor
Nano Multiple layer coating

## Slide 4
Single Layer
Multi-Layer
HSX/HGX coating- Multiple layer Coating

## Slide 5
Edge Treatment
Cutting edge without treatment
Tougher cutting edges
Sharper cutting edges
Relief face
Rake face
Cutting edge
with treatment

## Slide 6
HGX Overview

## Slide 7
Machine：HSK A63 spindle
Cutter： R4x2t Ball nose
Material：1.2312 33HRC
Cutting： flat face finishing
Coolant： Emulsion
Vc： 200 m/min
n： 8000 rpm
fz： 0,187mm/t
Vf： 3000mm/min
ap： 0,08mm
ae： 0,2mm
After
6 hours
After
9 hours
H company
HGXB20800875
Successful Story – HGXB2- Internal Test

## Slide 8
HGXB 2080 0874
H Competitor
H Competitor
HGXB2080 0875
After 10h36min
Machine: QJM AV612
Cutter: R4 Ball nose
Material: 1.2311 33HRC
Cutting：3D finishing
Coolant: Emulsion
Vc： 200 m/min
n： 8000
fz： 0,188mm/t
Vf： 3000mm/min
ap： 0,05mm
ae： 0,2mm
After 14h
Machine: QJM AV612
Cutter: R4 Ball nose
Material: 1.2311 33HRC
Cutting：3D finishing
Coolant: Emulsion
Vc： 214 m/min
n： 8500
fz： 0,2mm/t
Vf： 3500mm/min
ap： 0,08mm
ae： 0,15mm
Successful Story – HGXB2 – Internal Test

## Slide 9
Machine: HSK A63
Cutter: R6 Ball nose
Material: 1.2714 46HRC
Cutting：3D finishing
Coolant: Emulsion
Vc： 250 m/min
N: 6634rpm
fz： 0,11mm/t
Vf : 1500mm/min
ap： 0,36mm
ae： 0,36mm
Kunden Kommentar
Very shining surface and even after 10 hours milling,
There was almost no obvious wear.
HGXB2120
575min
Successful Story – HGXB2 - Germany

## Slide 10
Machine: MT CUT
Cutter: R3 Ball nose
Material: 1.2312
Cutting：Z constant finishing
Vc： 250 m/min
N: 13269rpm
fz： 0,07mm/t
Vf: 1857mm/min
ap： 0,1mm
ae： 0,15mm
Successful Story - HGXB2 - Germany
Kunden Kommentar
Long tool life and excellent finishing quality
HGXB2060 0660
420min

## Slide 11
HGXR4080R2,0 0875
Machine：DMC 635V (HSK63)
Cutter： D8xR2 Radius endmill
Material：1,2379 40HRC
Cutting： Finishing
Coolant： Emulsion
Customer Comments:
Even after 7 hours finishing application,
Still very sharp and more than twice tool life of current competitor.
This end mill is multiple tasking, not only
Z constant milling and side milling, slotting.
Successful Story – HGXR4 - Germany
M Company

## Slide 12
Machine：Quick Jet V70S
Holder： E50
Cutter： D6xR0,5x4t Radius Endmill
Material：1,2738HH, HRC46-48
Cutting： Z constant semi finishing
Coolant： Emulsion
Vc： 135 m/min
n： 7200 rpm
fz： 0,083mm/t
Vf： 2400mm/min
Ap: 0,03mm
Ae: 0,1mm
HGXR4060R0.5 0650
4 hours
Successful Story – HGXR4- Poland

## Slide 13
Machine：Makino V33
Cutter： D4xR2x2t ball nose Endmill
Material：1.2083, HRC48-50
Cutting： Z constant semi finishing
Coolant： Emulsion
Vc： 113 m/min
n： 9000 rpm
fz： 0,11mm/t
Vf： 2000mm/min
Ap: 0,03mm
Ae: 0,1mm
After 25 hours 18 minutes
Successful Story – HGXB2 - Germany