## Slide 1
Miniature Deep End Mill
Notes: Sustained Growth Smart Optimization

## Slide 2
Item Code
L8
Under neck length

## Slide 3
Item Code

## Slide 4
Deep Series

## Slide 5
Features – Water Drop Geometry
D<1mm
D>1mm
deflection
Water drop geometry for small diameter avoids excessive contact of cutting edge and workpiece during deflection
Deflection caused by cutting force

## Slide 6
Products – Precision R0.05mm
N company
M***230
H company
EP***2001
U company
H***2001
HGXB2001 0450 P

## Slide 7
Products – Precision R0,15mm
N company
M***230
H company
EP***2003
U company
H***2003
HGXB2003 0450 P

## Slide 8
High Precision
Diameter＜1mm
+/-0.003mm (+/-0.0015mm)
1mm≤Diameter≤12mm
+/-0.005mm
Diameter＞12mm
+/-0.008mm
All in range
Out of range
Two side out of range
H company
Z company
Radius Tolerance

## Slide 9
Products - Precision
HGXB2001L0.2 0450 (R0.05mm Ball nose)
Tolerance: -0.002/+0.001mm
HGXB2002L1 0450 ( R0.1mm Ball nose)
Tolerance: -0.002/+0.002mm
Notes: The mill’s ball nose accuracy can be controlled between R ± 0.0015 mm.

## Slide 10
Vc： 75 m/min
n： 12000 rpm
fz： 0,03mm/t
Vf： 1500mm/min
ap： 0,06mm
ae： 0,03mm
Machine：Quick Jet 1612
Holder： HSK63 – SKL2
Cutter： D2xR0.2xL10
Material：1.2083ESR HRC50
Cutting： Finishing
Coolant： Emulsion
HSXR2020R0.2L10 (after 600m)
J Company 4J***020002080 (after 400m)
Successful Story – HSXR2L

## Slide 11
Vc： 80 m/min
n： 12700 rpm
fz： 0.03mm/t
Vf： 760mm/min
ap： 0.03mm
ae： 2mm-0.2mm
Machine：Makino
Holder： PowRgrip. HSK63
Cutter： D2xL20
Material：1.2343ESR HRC52
Cutting： Z constant slotting
Coolant： Emulsion
HSXE2020L10 0450
Customer Comments:
We tested the following items for comparison
SGSO HSXE2020L10 0450
H company E****-2020-10-ATH
N company M**230 08-00200-20100
There is no big difference in tool wear, but SGSO created much better tolerance in width of ribs.
Machine Time: 90min
Successful Story – HSXE2L

## Slide 12
Machine：Roeders
Holder： PowRgrip. HSK40E
Cutter： D1xR0,5xL4
D2xR1xL6
Material：1.2343ESR HRC54
Cutting： Z constant
Coolant： Airblow
HSXB2020L6 0450
HSXB2010L4 0450
Customer Comments:
We compared SGSO with H company MR***230SF, finally SGSO reached smaller wear and the surface quality after finishing is also better than competitor
Successful Story – HSXB2L

## Slide 13
HSXB2030L16 0660
Machine：GF HPM80
Cutter： R1,5xL16 Ball nose
Material：DAC Magic 48HRC
Cutting： Copy milling
Coolant： Airblow
Vc： 130 m/min
n： 14000 rpm
fz： 0,057mm/t
Vf： 1600mm/min
ap： 0,1mm
ae： 0,1mm
Customer Comments:
After more than three hours using,
There is still very small wear, possible
For further using. Much better than current competitor
Cutting Time 192 min
Successful Story – HSXB2L

## Slide 14
Successful Story – HGXB2L
Machine：Quickjet AV70S
Holder： MST HSK E50-SLRA4
Cutter： R0.25xL2 Ball nose
Material：1.2343ESR HRC50-52
Cutting： 15°&45° slope face finishing
Coolant： Emulsion
Vc： 40 m/min
n： 25000 rpm
fz： 0,01mm/t
Vf： 500mm/min
ap： 0,01mm
ae： 0,025mm
15° face
45° face
Wear after 7hours
N company
O company
HGXB2005L2 0450

## Slide 15
Successful Story – HGXB2L
Machine：Makino IQ500
Holder： HSK-E32-SLRA4-22
Cutter： R0.1xL1 Ball nose
Material：X36CrMo17 (1.2316) HRC52
Cutting： Z constant finishing
Coolant： Emulsion
Vc： 22.6 m/min
n： 36000 rpm
fz： 0,004mm/t
Vf： 300mm/min
ap： 0,01mm
ae： 0,02mm
N company
HGXB2002L1 0450
After 1,5 hours
After 14 hours

## Slide 16
Machine：Makino AV70S
Holder： HSK E50
Cutter： R0,25xL2 Ball nose
Material：1,2343ESR, HRC50
Cutting： Z constant semi finishing
Coolant： Emulsion
Vc： 157 m/min
n： 25000 rpm
fz： 0,01mm/t
Vf： 500mm/min
Ap: 0,01mm
Ae: 0,025mm
Successful Story – HGXB2L
H company
HGXB2005L2 0450
3,5 hours

## Slide 17
Machine：Quickjet AV70S
Holder： MST HSK E50-SLRA4
Cutter： R0.25xL2 Ball nose
Material：1.2343 HRC50-52
Cutting： 10° slope face finishing
Coolant： Emulsion
Successful Story – HGXB2L
HGXB2005L2 0450
After 120min
Vc： 40 m/min
n： 25000 rpm
fz： 0,01mm/t
Vf： 500mm/min
ap： 0,01mm
ae： 0,025mm
M***230-R025*2
After 60min
Machined surface
After 120min
Machined surface
After 60min
N company

## Slide 18
Machine：Makino V56I
Holder： MST HSK A63-SLRK12
Cutter： D0.8xR0.05xL6 Radius
Material：1.2083 HRC50-52
Cutting： Z constant finishing
Coolant： Emulsion
Vc： 45 m/min
n： 18000 rpm
fz： 0,008mm/t
Vf： 300mm/min
ap： 0,02mm
ae： 0,01mm
Successful Story – HGXR2L
Competitor N 1st pcs 180min
SGSO 1st pcs 180min
SGSO 2nd pcs 180min
HGXR2008R0.05L6 0450
HGXR2008R0.05L6 0450
Competitor N